## Slide 1: Optimizing Your Process Through Lignin Management
Sandy Beder-Miller
Senior Applications Specialist
Rick Van Fleet
Fiber Line Business
Development Manager
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Optimizing Your Process Through Lignin Management
Sandy Beder-Miller
Senior Applications Specialist
Rick Van Fleet
Fiber Line Business
Development Manager

## Slide 2: Presenter: Brad S. Carlberg, P.E., CSE
Brad S. Carlberg is a Consulting Engineer for BSC Engineering & a registered, Professional Control Systems Engineer with over thirty years’ experience in Process Control Engineering specifically with Distributed Control Systems, Programmable Logic Controllers, and Human Machine Interfaces combining extensive experience with both Hardware and Software Design, Programming, Implementation and Startup, including Advanced Continuous and Batch Control Programming.
Brad received his B.S. in Mechanical Engineering in February, 1984 from Washington State University in Pullman, WA.
He joined ISA in 1986 and is a Senior Member.
His hobbies include distance running, jazz and blues music, and flying his 1946 Ercoupe 415C Light Sport airplane.
Brad maintains his home office in Hoodsport, WA on the Olympic Peninsula & his airplane hangar at the Richland airport (KRLD).
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Brad S. Carlberg is a Consulting Engineer for BSC Engineering & a registered, Professional Control Systems Engineer with over thirty years’ experience in Process Control Engineering specifically with Distributed Control Systems, Programmable Logic Controllers, and Human Machine Interfaces combining extensive experience with both Hardware and Software Design, Programming, Implementation and Startup, including Advanced Continuous and Batch Control Programming.
Brad received his B.S. in Mechanical Engineering in February, 1984 from Washington State University in Pullman, WA.
He joined ISA in 1986 and is a Senior Member.
His hobbies include distance running, jazz and blues music, and flying his 1946 Ercoupe 415C Light Sport airplane.
Brad maintains his home office in Hoodsport, WA on the Olympic Peninsula & his airplane hangar at the Richland airport (KRLD).

## Slide 3: Authors: Sandy Beder-Miller & Rick Van Fleet
Sandy Beder-Miller has a Bachelor of Science in Forestry from University of Massachusetts (1977) and a Masters of Statistics (1979) from North Carolina State University. Upon graduation Sandy has worked as a Biometrician for Crown Zellerbach in their Forestry Research Group and held positions in computer programming with Kidd Creek Mines Ltd. in Timmins, Ontario; MINITAB Statistical Software as a Program Developer; and as a Statistician for the U.S. EPA in Duluth Minnesota.
She came to the pulp and paper industry in 1988 to work as a programmer for Potlatch in their Cloquet, Minnesota mill. After 2 years of supporting the mill’s production management software and roll tracking system, Sandy applied for a job as a Pulp Mill Relief Supervisor and earned her Pulp and Paper “degree” through 5 years of grave yard shifts. In 1996, she became a Bleach Plant Production Engineer for Boise Cascade’s Wallula, Washington mill and also worked on W3 Paper Machine as an Additives Coordinator, part time Shift Supervisor and Dry End Day Supervisor. Sandy began working for BTG in May of 2000 as a Senior Applications Specialist traveling North and South America specializing in bleaching applications and also serves on BTG’s global fiber line team.
Sandy has been married for 35 years to Larry Miller, a Forest Geneticist. Together they have raised 3 daughters Laura (35), Paula (33) and Abigail (30). They now reside in Yaak, Montana.
Rick Van Fleet has been a Fiberline Business Development Manager at BTG Americas, Inc. since March, 2013 specializing in Pulping Process Control. He has conducted studies and implemented pulping process control projects in 20+ countries; and his specialties include process analysis, economic projections, justification of automation systems, managing change with operators.
Prior to joining BTG, Rick spent twenty years with Honeywell in Phoenix, AZ holding several titles including Product Manager, Global Strategic Marketing Solutions Leader- Pulping Honeywell Process Solutions - July 2011 – January 2013 (1 year 7 months),
Global Advanced Controls Consultant Lead, Pulping Product Manager (Honeywell-Measurex) 1997 – 2000 (3 years), Advanced Controls Consultant (Honeywell Process Solutions), 1993 – September 1998 (5 years)
Before joining Honeywell, Rick was Manager of Software Products for Instrument Control Services in Pensacola, FL & Manager Pulp and Paper for C S technologies, Inc. in Poughkeepsie, NY. Rick began his career as Bleach Plant Process Engineer for Great Lakes Forest Products in Dryden, Ontario in 1983 after receiving his B.S in Chemical Engineering from the University of Waterloo.
Rick maintains his home office in Cave Creek, AZ with his wife, Laurie; their two daughters, Aaren (24) & Sierra (20), attend Western Ontario University.
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Sandy Beder-Miller has a Bachelor of Science in Forestry from University of Massachusetts (1977) and a Masters of Statistics (1979) from North Carolina State University. Upon graduation Sandy has worked as a Biometrician for Crown Zellerbach in their Forestry Research Group and held positions in computer programming with Kidd Creek Mines Ltd. in Timmins, Ontario; MINITAB Statistical Software as a Program Developer; and as a Statistician for the U.S. EPA in Duluth Minnesota.
She came to the pulp and paper industry in 1988 to work as a programmer for Potlatch in their Cloquet, Minnesota mill. After 2 years of supporting the mill’s production management software and roll tracking system, Sandy applied for a job as a Pulp Mill Relief Supervisor and earned her Pulp and Paper “degree” through 5 years of grave yard shifts. In 1996, she became a Bleach Plant Production Engineer for Boise Cascade’s Wallula, Washington mill and also worked on W3 Paper Machine as an Additives Coordinator, part time Shift Supervisor and Dry End Day Supervisor. Sandy began working for BTG in May of 2000 as a Senior Applications Specialist traveling North and South America specializing in bleaching applications and also serves on BTG’s global fiber line team.
Sandy has been married for 35 years to Larry Miller, a Forest Geneticist. Together they have raised 3 daughters Laura (35), Paula (33) and Abigail (30). They now reside in Yaak, Montana.
Rick Van Fleet has been a Fiberline Business Development Manager at BTG Americas, Inc. since March, 2013 specializing in Pulping Process Control. He has conducted studies and implemented pulping process control projects in 20+ countries; and his specialties include process analysis, economic projections, justification of automation systems, managing change with operators.
Prior to joining BTG, Rick spent twenty years with Honeywell in Phoenix, AZ holding several titles including Product Manager, Global Strategic Marketing Solutions Leader- Pulping Honeywell Process Solutions - July 2011 – January 2013 (1 year 7 months),
Global Advanced Controls Consultant Lead, Pulping Product Manager (Honeywell-Measurex) 1997 – 2000 (3 years), Advanced Controls Consultant (Honeywell Process Solutions), 1993 – September 1998 (5 years)
Before joining Honeywell, Rick was Manager of Software Products for Instrument Control Services in Pensacola, FL & Manager Pulp and Paper for C S technologies, Inc. in Poughkeepsie, NY. Rick began his career as Bleach Plant Process Engineer for Great Lakes Forest Products in Dryden, Ontario in 1983 after receiving his B.S in Chemical Engineering from the University of Waterloo.
Rick maintains his home office in Cave Creek, AZ with his wife, Laurie; their two daughters, Aaren (24) & Sierra (20), attend Western Ontario University.

## Slide 4: Lignin is the “glue” that holds the wood chip together.
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Removing lignin is a very necessary but costly part of the pulping process.
Therefore having state-of the-art measurements and control capabilities are extremely important in maximizing business performance and final pulp quality.
It has been a constant challenge to accurately and reliably measure lignin from the blow line through the bleach plant.
The industry has relied on laboratory measurements, and/or slower multi-point kappa analyzers to measure fiber kappa.
An oftentimes equally important but neglected component is the dissolved (or filtrate) lignin moving through the process, which also can widely vary and consume a significant portion of bleaching chemicals.
With these critical measurements being problematic, new innovative technologies have been developed to enhance the ability to optimize the pulping process and deliver significant sustainable gains in business performance for the industry.
This paper will discuss the recent improvements in measuring fiber and filtrate lignin on-line and its impact on fiber line and bleach plant controls.
Figure 1 is a conceptual diagram of lignin and brightness from the blow line through the bleach plant.
The amount of lignin quickly reduces as we move through the bleach plant, while the brightness increases.
The addition of extended cooking and oxygen delignification ahead of the bleach plant lowers the Kappa entering the bleach plant.
Thus, Brightness may be a better measurement at the post extraction stage due to the very low Kappa numbers.
Prior to the extraction stage, we focus on kappa measurement.
Before online Kappa measurements were available, mills relied on a tester to run a test every 2 hours.
Lignin is the “glue” that holds the wood chip together. Chemical pulping relies on efficiently separating wood fibers from lignin. The most common measurement of lignin is the Kappa Number, which we can measure in the laboratory.
Chemical pulping relies on efficiently separating wood fibers from lignin.

## Slide 5: Example of MultiPoint Kappa Analyzer
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: When Kappa analyzers became commercially available in the early 1990’s, Kappa Number (Kappa) has been measured on-line. Kappa is defined as the milliliters of 01N potassium permanganate solution consumed by 1 g of dry pulp using a standard laboratory procedure. For example, consider the amount of lignin in a 30 kappa softwood pulp. After the digester, the pulp has been delignified by 90 percent. The remaining 10 percent of lignin in the pulp is the focus of measurement and control after the blow line.

## Slide 6: Variability Associated with the Kappa Number
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: However, there can be numerous problems associated with the manual kappa test due to sample preparation, chemical strength, and method of titration.
Testing and sampling error is a part of the Kappa variability from the digester, as shown in Figure 3.
The Kappa result is used to make changes in digester cooking, control the Oxygen Delignification stage, and to cut or increase chemical to the bleach plant.

## Slide 7: What are we measuring today??
O2 Delignified Pulp
Black
Liquor
Unbleached Fibers
Dissolved
Lignin
Fiber Bound
Lignin
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Until recently there have not been direct measurements of dissolved lignin and total bleach load.
Operators have relied on surrogate values such as conductivity or chemical residual to account for black lignin carryover.
Inaccurate measurement of dissolved lignin can lead to overuse of bleaching chemicals and increased costs to the operation.

## Slide 8: True Measurement of Lignin in Filtrate
PaperWeek 2014 “Is Conductivity the
Best Measurement of Carryover?”
Andersson et al
DLT
Kappa Analyzer
O2 Delignified Pulp
Black
Liquor
Unbleached Fibers
Dissolved
Lignin
Fiber Bound
Lignin
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Fiber lignin is not the only lignin in the process pipeline.
Oxygen delignified pulp is comprised of fiber bound lignin and inorganic and organic compounds, commonly referred to as black liquor or dissolved lignin.
The Kappa analyzer washes away the black liquor in its processing of the online sample, leaving the bleach plant operator to estimate what other compounds are entering the plant.
Mills struggle with proper washing in the brown stock area; they must balance the cleanliness of the pulp they are sending to the bleach plant along with the amount of solids they are sending to the evaporators.
When the washing is poor, the challenge in the bleach plant operation is to accurately quantify the amount of black liquor carryover, because it affects the first stage of processing.
At present, most mills rely on conductivity or chemical residual after chlorine dioxide addition to indicate carryover. These are at best surrogate measurements in place of quantifying dissolved lignin.
Dirty pulp entering the bleach plant with an excess of dissolved lignin will consume chlorine dioxide that is used to remove the lignin in the fiber in the first stage.
Andersson et al2 have shown through mill testing that the correlation of COD and conductivity is poor, as shown in the Figure 9 trend. This may lead to incorrect decisions in raising or lowering shower flows in the brown stock washing area, dosing chemical in the bleach plant, or both.

## Slide 9: Why do we measure fiber lignin?
Digester Control
– Increase yield by cooking to a higher kappa
Oxygen Delignification Control
– Make our target
Bleach Plant
– Measure carry over
– Control Chemical Dosage in the D0 stage
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Yield increases of 0.5% to 2.0% are possible when the digester Kappa setpoint increases
After the digester, the pulp has been delignified by 90 percent. The remaining 10 percent of lignin in the pulp is the focus of measurement and control after the blow line.
Testing and sampling error is a part of the Kappa variability from the digester
The Kappa result is used to make changes in digester cooking, control the Oxygen Delignification stage, and to cut or increase chemical to the bleach plant.
Typically, operators will cook to a lower kappa to avoid discharging uncooked pulp. Overcooking leads to yield losses from the digester and higher production costs. More frequent kappa updates to the cooking control can lead to reduced variability and allow the mill to confidently raise their Kappa targets.

## Slide 10: Measuring Fiber Lignin
Manual Testing
Central Analyzer`
Single Point Analyzer
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: As such, some mills elect to measure Kappa manually, resulting in variable results and erratic update times. Operators are often reluctant to make digester changes b
Existing on-line technology has focused on the multi-point analyzer since the early 1990’s. The device automatically samples and transports the pulp to a central analyzer. The central analyzer screens, washes, and measures Kappa.ased on infrequent samples.
There is available technology to measure both fiber and filtrate lignin using single point analyzers and in-line sensors.
A new single point analyzer is now available that is mounted directly to the pulp processing pipeline. This analyzer contains all unit operations of the traditional multi-point Kappa analyzer, such as pulp sampling, screening, washing, and optical measurement of Kappa

## Slide 11: Kappa Analyzer
Screening
Washing
Measurement
Reporting
Functions
Advantages
Disadvantages
Remove Lab Bias
Test is performed the same way every time
Long distance from sampler to central analyzer
Slow update time to DCS
Maintenance requirement is high
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA

## Slide 12: Multi-Point Kappa Analyzer: Total Cost of Ownership
~ $250K US
Installation Cost
Annual Service Contract
Spare Parts
Ongoing supplier support
+ Local E&I oversight
UV Lamp once per year
Valve Rebuild Kits
Agitator motors, parts
Site Preparation
Water (filtering, heating)
Air
Enclosure (site preference)
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Existing on-line technology has focused on the multi-point analyzer since the early 1990’s.
The device automatically samples and transports the pulp to a central analyzer.
The central analyzer screens, washes, and measures Kappa.
The measurement is based on the use of UV light passed through a diluted pulp sample of well washed pulp.
The analyzer uses an optical measuring method to determine the amount of lignin in the pulp.
This method has been shown to correlate well with the results of laboratory chemical Kappa tests over a wide Kappa Number range, for a range of different wood species.
The analyzer consistently and repeatedly takes the measurement, eliminating differences between testers.
Negatives associated with the analyzer are the high cost of installation, which can be up to $250,000. Under optimal conditions, the traditional Kappa analyzer can process 4 to 6 samples per hour across up to 8 sample points, such as the digester blow line, pre and post oxygen delignification, feed to the bleach plant, and post extraction stage in the bleach plant.
However, large gaps in Kappa updating to the DCS may occur because the analyzer must divide its processing time between samples.
Mill control strategies may be affected by sporadic updating, and process changes may be missed due to long intervals between samples.
Utilizing an eight point Kappa analyzer in unbleached Kraft applications requiring measurement of only one or two sample points is cost prohibitive.
As such, some mills elect to measure Kappa manually, resulting in variable results and erratic update times.
Operators are often reluctant to make digester changes based on infrequent samples.
Automated control is not possible with the infrequent laboratory Kappa updates.
Typically, operators will cook to a lower kappa to avoid discharging uncooked pulp.
Overcooking leads to yield losses from the digester and higher production costs.
More frequent kappa updates to the cooking control can lead to reduced variability and allow the mill to confidently raise their Kappa targets.
Hart, Peter W. And Rudie, Alan W. (Editors). ”The Bleaching of Pulp 5th Editon”. TAPPI PRESS, Altanta, GA, (2012).

## Slide 13
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Single-point Kappa analyzer requires less approach piping because the sensor is direct-mounted on the pipe
Single-point Kappa analyzer uses less water because of this
Consistency is self-correcting, self-adjusting

## Slide 14: Installation of Single Point Kappa Analyzer
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: A new single point analyzer is now available that is mounted directly to the pulp processing pipeline.
This analyzer contains all unit operations of the traditional multi-point Kappa analyzer, such as pulp sampling, screening, washing, and optical measurement of Kappa.
Because of the single sample point, Kappa measurements for all fiber line applications are updated more promptly.
The single point concept allows for incremental investment in key positions for mills with limited capital.
It is now possible to update 12 samples per hour for a continuous digester, and 2 to 3 samples per blow for batch digesters.
The single point Kappa analyzer can also be placed pre- and post- Oxygen Delignification or in the bleach plant to control the dosage of chlorine dioxide.
SBK Blowline
DLT O2 Delig & BSW
BLT Bleach Plant

## Slide 15: Pulping Control Benefits
Allows for individual adjustments of Chemical to Wood ratio and/or
H-factor targets
Can be on a Grade Recipe or Digester basis
Yield increases of 0.5% - 2.0% possible
Batch Digesters
O2 Delignification & Bleaching
Faster update and increased % uptime for tighter
kappa factor control and optimization of chemicals
Faster update means 2-3 samples per blow
Continuous Digesters
Up to 12 samples per hour
Allows for quicker coordinated adjustments of temperature & management of cooking zone
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Never been done before – Tune Digester cooking model for individual vessels
If each blow takes about 30 minutes to empty – 2 – 3 samples / blow/ digester

## Slide 16
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: An example from a southern unbleached Kraft mill running approximately 800 tons per day demonstrates how an affordable single point solution reduced Kappa variability and raised operator confidence in Kappa measurement.
Green Bay Packaging in Morrilton, Arkansas has relied on laboratory kappa samples taken every 2 hours.

## Slide 17: Kappa Shift Increases Yield:
Green Bay Packaging Morrilton - 800 TPD Brown Mill
Typical Kappa range 91 to 101
2.96 increase in Blow line Kappa
Currently verifying reduced chip usage/increased yield
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Figure 5 shows the rise in Kappa values after automating sampling and testing was installed.
The 2.96 increase in Kappa roughly translates to a potential increase in yield that is now being verified by the mill.
Green Bay Packaging has also seen a 29% reduction in Kappa standard deviation as shown in Figure 6.
Operators are also making fewer changes to the alkali-to-wood ratio due to more frequent Kappa updates.

## Slide 18: Less Manipulation of Alkali to Wood Ratio
Alkali/Wood Ratio | Before SPK | After SPK
Ratio Changes | 253 | 133
Average Ratio | 13.60 | 13.16
Standard Deviation | 0.59 | 0.31
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Figure 7 shows that operators made 47% fewer corrections which in turn have resulted in lower Kappa variation out of the digester.

## Slide 19: Benefits of Automated Testing Seen By Green Bay Packaging Morrilton
29% Reduction in Kappa Standard deviation
Operators have raised the kappa target; more confident in the result
47% reductions in changes to Alkali to Wood Ratio
Papermakers have a better indication of what is coming to the wet end
Eliminate unnecessary adjustments causing sheet breaks; 1 break = 36 minutes lost time
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: The Pulp Mill and Paper Mill Operations at Morrilton have accepted the new automated Kappa measurement and have cited many benefits of a single point automated kappa analyzer:
The sample point is now closer to the digesters so they can better adjust their cooks.
The control chart used to make changes in Alkali to Wood Ratio was only updated every 2 hours and is now updated every 30 minutes.
There are now less alkali-to-wood ratio changes. Previously, some changes were unnecessary and led to harmful kappa variability.
The operators are seeing a decrease in the daily standard deviation.
The operators raised the Kappa set point because they are more confident in the pulp mill's ability to control Kappa
Paper makers observe that they receive better and more timely data on the pulp that is coming to their machines. Manual Kappa samples were taken after the brown stock washers, which took 40 minutes per test. During this lengthy testing interval, the stock may have already reached the wet end of the paper machines. Usually, there was a one to two hour lag time in receiving test information
Paper makers can make preemptive moves to eliminate breaks from stock changes. One break causes 36 minutes of downtime. Previously, changes were made for anticipated off quality conditions that never materialized and the sheet broke due to the unnecessary process shift. This is currently being quantified.

## Slide 20: How can we measure everything in the pulp suspension???
Fiber lignin
Total lignin: Bleach Load
Filtrate lignin
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Fiber lignin is not the only lignin in the process pipeline.
Oxygen delignified pulp is comprised of fiber bound lignin and inorganic and organic compounds, commonly referred to as black liquor or dissolved lignin.
The Kappa analyzer washes away the black liquor in its processing of the online sample, leaving the bleach plant operator to estimate what other compounds are entering the plant.

## Slide 21: Bleach Load Measurement
O2 Delignified Pulp
Black
Liquor
Unbleached Fibers
Dissolved
Lignin
Fiber Bound
Lignin
Bleach
Load
Current measurement options
– Conductivity → indirect
– COD → laboratory, time, expensive
– Chemical residual → inline
– Kappa → discontinuous
Versus Bleach Load measurement
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Mills struggle with proper washing in the brown stock area; they must balance the cleanliness of the pulp they are sending to the bleach plant along with the amount of solids they are sending to the evaporators.
When the washing is poor, the challenge in the bleach plant operation is to accurately quantify the amount of black liquor carryover, because it affects the first stage of processing.

## Slide 22: Bleach Load Transmitter
UV technology similar to kappa analyzer, but in an LED & probe form
Measures fiber kappa and filtrate kappa to give the total bleaching demand
Optical Reflectance Measurement
5 LEDs in the sensor
–Blue
–Red
–Green
–UV
–NIR
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: There are times when it is not necessary to separate the fiber and filtrate lignin and only report a total sum of the two components.
VanFleet has developed and defined the measurement of “Bleach Load” where the fiber and filtrate kappa is measured in an on-line sensor and used in Kappa factor control.
The laboratory procedure to measure bleach load involves running a fiber Kappa test, consistency, and filtrate Kappa from the pulp squeezings of the sample.
Van Fleet Rick, Morningred, Dune, Podasak, Steve, Beder-Miller, Sandra. ”Bleach Load: A New Sensor Based Improvement for Bleach Plant Advanced Control”. International Bleaching Conference. Portland Oregon, September, 2011.
The LED vs. the traditional lamp requires less frequent replacement – who knows really how long the LED will last

## Slide 23: How to Measure Bleach Load:
1. Measure Consistency of the sample
2. Fiber kappa test (lignin per gram of fiber)
3. Kappa test on the filtrate (lignin per grams of filtrate)
4. Add the two results to compute “Bleach Load”
Use Bleach Load to develop a mathematical relationship between the sensor signals and the lab test
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Total bleach load includes the carryover entering the bleach plant so the chlorine dioxide dosage is adjusted before the chemical is added.
This removes the guesswork where the operator would adjust a ”bias” or add more chlorine dioxide to account for the amount of estimated carryover coming into the bleach plant.
In a North American bleach plant, the bleach load measurement was used to help control the first stage of the bleaching operation.
The filtrate Kappa is converted to a gram equivalent of the filtrate in the pulp suspension.
The fiber and filtrate Kappa tests reported in grams are added together.

## Slide 24: Suggested Sensor Placement for Control Strategy at D100
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA

## Slide 25: Bleach Load Calibration at Feed to Bleach
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA

## Slide 26: Using Bleach Load In Existing D100 Control USA Mid West Mill
Uses D100 Brightness after chemical addition for feedback adjustment
Kappa Factor calculated but not used
Savings of $60K per year without additional improvements to existing mill control!
Mill Control Notes:
 | Tons Per Day | Bleach Load | Kappa Factor | % ClO2 Applied | Operator Bias
Before | 522 | 18.52 | 0.232 | 1.64 | 0.651
After | 461 | 18.27 | 0.231 | 1.60 | 0.000
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: The chart in Figure 13 shows the overall lowering of chlorine dioxide usage.
This is due to the elimination of operator bias from the existing compensated brightness control and resulted in an annual saving of $60K US.
The operator was able to achieve his target because the dissolved lignin was measured along with the fiber Kappa before chlorine dioxide was dosed

## Slide 27: Reduce Chlorine Dioxide Using Bleach Load in Control
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Figure 14 shows a trend of the percent chlorine dioxide applied when bleach load is used versus the traditional fiber Kappa measurement.
Additional savings are possible with improvement of the existing control strategy.
The Bleach Load Transmitter operates with five LEDs; blue, red, green, NIR, and UV, and works under the principle of optical reflection.
Laboratory samples are collected along with raw LED values.
The raw signals are used in combination to predict Bleach load.
The number of signals used in the calibration will vary depending on the process and location of the bleach load sensor.

## Slide 28: Bleach Load Calibration Post Extraction
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Figure 15 is an example of a calibration and is using the red and UV LED in the model.
The Bleach Load Transmitter is usually installed in the first stage of the bleach plant and post extraction.
Because the transmitter is measuring both fiber and filtrate, it can uncover problems in bleach plant washing.
Poor washing has been shown to lead to higher percent of filtrate Kappa due to carryover of filtrate from the washer. In the example shown in Figure 15

## Slide 29: Filtrate Contribution to Total Bleach Load
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA

## Slide 30: Filtrate Contribution to Total Bleach Load
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: Figure 16, the mill acknowledged they were having problems washing the extraction filtrate from the pulp in a three stage bleach plant.
This caused excessive use of chlorine dioxide in the brightening stage.
Laboratory testing revealed that the filtrate kappa was over 35% of the total bleach load.
Adjustments were made to the washer showers, resulting in an almost 15 percent reduction in filtrate Kappa.
A traditional multi-point analyzer would have missed this and extended troubleshooting time to determine why more chlorine dioxide was needed for the first brightening stage.

## Slide 31: Conclusions
Technology exists for on-line measurement of lignin
Replaces slow, analyzers/inaccurate manual tests
This technology has been used to:
Aid in Digester Control
Identify Washer Issues
Dilution Factor Control
Measure Carryover to the Bleach Plant
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA
Notes: There is available technology to measure both fiber and filtrate lignin using single point analyzers and in-line sensors.
This is a significant change from the multi-point analyzers that can be maintenance intensive, require high installation costs, and have inadequate uptime times for sound process control.
The dissolved lignin and total bleach load sensors are in-line probes that can be retracted while the process is running, providing continuous updates.
Dissolved lignin in the filtrate can now be measured using a UV light source, which is the same measuring source as in the traditional fiber kappa analyzer.
The third sensor discussed, the Bleach Load Transmitter, measured fiber and filtrate in a combined signal using optical reflectance and LED technology to determine total Bleach Load.
Bleach Load represents the total chlorine dioxide demand to the bleach plant and allows the elimination of operator bias which often results in bleaching chemical overuse.
Removing lignin is a very necessary but costly part of the pulping process.
Therefore having state-of the-art measurements and control capabilities are extremely important in maximizing business performance and final pulp quality.
It has been a constant challenge to accurately and reliably measure lignin from the blow line through the bleach plant.
The industry has relied on laboratory measurements, and/or slower multi-point kappa analyzers to measure fiber kappa.
An oftentimes equally important but neglected component is the dissolved (or filtrate) lignin moving through the process, which also can widely vary and consume a significant portion of bleaching chemicals.
With these critical measurements being problematic, new innovative technologies have been developed to enhance the ability to optimize the pulping process and deliver significant sustainable gains in business performance for the industry.
This paper will discuss the recent improvements in measuring fiber and filtrate lignin on-line and its impact on fiber line and bleach plant controls.

## Slide 32: Thank You!
sandy.beder-miller@btg.com
+1 678-488-8138
rick.vanfleet@btg.com
+1 602-316-6774
brad.carlberg@bsc-engineering.com
+1 251-454-1200
Process Control & Safety
Symposium 2015
9-12 November
Houston, Texas USA